## Slide 1
Energy-efficient nanoelectronics using giant spin-orbit materials
Comprehensive Viva
Priyesh Kumar
Roll: 1910705, Email: priyesh19@iiserb.ac.in
Electrical Engineering and Computer Science (EECS) Dept.
Indian Institute of Science Education and Research (IISER) Bhopal
Advisor: Dr. Kuntal Roy, Email: kuntal@iiserb.ac.in
27 August 2021

## Slide 2: Contents
Introduction
  Spintronics and nanomagnetics
  Magnetic anisotropy
  Magneto-resistance
  Magnetization dynamics
  Switching using magnetic field
  Spin-transfer-torque
  Spin Hall effect and spin-orbit-torque
  Ferromagnetic resonance and spin pumping
Plan of works
  Probing the resistivity of ultra-thin spin-orbit materials
  Spin-torque ferromagnetic resonance
  Switch magnetization using spin-orbit-torque
Experimental
  Electron beam lithography (EBL) and scanning electron microscope (SEM)
  Transmission electron microscope (TEM)
  Atomic/Magnetic force microscope (AFM/MFM)
  Ferromagnetic resonance (FMR)
  Vibrating sample magnetometer (VSM)
  Electrical characterization using probe station and accessories
  Four-probe setup
  Signal generator, oscilloscope, spectrum analyser, bias-tee and power supply
  X-Ray diffraction (XRD)
  Sputtering

## Slide 3: Electronics: Development and Future
Issues
Energy dissipation
Process variation
Moore’s Law
Gordon Moore
Intel Co-Founder
Number of transistors
DOUBLES in every TWO years
Transistor counts 1970-2018 & Moore’s Law
Transistor as a
binary switch
Notes: Line edge and random dopant fluctuation
Density doubles in every two years, number of transistor per unit area

## Slide 4: Electronics: Development and Future
Issues
Energy dissipation
Process variation
Moore’s Law
Gordon Moore
Intel Co-Founder
Number of transistors
DOUBLES in every TWO years
Transistor counts 1970-2018 & Moore’s Law
Transistor as a
binary switch
Bohr: Our research group has screened some of these options. This will not only help Intel, but it will help the university research groups identify the more promising options that we should collectively invest in. It may change as more researchers weigh in, but the conclusion at this point is that spintronics may have better chance in the future.
Mark Bohr, a senior fellow at Intel
http://semiengineering.com/one-on-one-mark-bohr/ (2014)
Notes: Line edge and random dopant fluctuation
Density doubles in every two years, number of transistor per unit area

## Slide 5: Spintronics: Spin-Electronics
Spin
Electron
Charge
Apart from having charge, an electron has spin
Up/Down 0/1 (binary information)
E barrier
A rapidly developing nanotechnology
  Store, non-volatile
  Process
  Communicate
  In-built functionality
No charge movement, rotation of spin
  No ohmic dissipation, but dissipation due to damping
There is dissipation due to applying charge voltage/current
Key Issue
Notes: Spin is the intrinsic angular momentum of an elementary particle as being the result of its rotation about its own axis
In Spintronics, information is stored and transmitted using another property of electrons called spin.
Electrons moving through a nonmagnetic material normally have random spins, so the net effect is zero. External magnetic fields can be applied so that the spins are aligned (all up or all down), allowing a new way to store binary data in the form of one’s (all spins up) and zeroes (all spins down).

## Slide 6: Single-domain nanomagnets
W.F. Brown Jr.,
The fundamental theorem of the ferromagnetic particle theory
Magnetic domain formation should be limited to very small dimensions (100 nm) because of the competition between the magnetostatic energy and the quantum-mechanical exchange energy, causing nanomagnets to behave like single giant spins.
Electron beam lithography (EBL)
Exchange interaction
  Pauli’s exclusion principle
  Coulomb repulsion
Each electron small magnet
  Ferromagnet
  Ferrimagnet
  Antiferromagnet
Notes: Single domain nanomagnets are formed due to exchange interaction, which is a simultaneous action of Pauli’s exclusion principle and Coulomb repulsion.

## Slide 7: Macrospin/Giant spin
All the spins rotate in unison

## Slide 8: Charge current versus spin current
Charge current
Spin-polarized current
Pure spin current
Charge
Spin
Spin-orbit coupling
Pt, Ta, W, CuBi
Charge current = 8
Spin current = 0
Charge current = 6
Spin current = 2
Charge current = 0
Spin current = 2
Js
Notes: Here I am going to present similarities and differences between charge current and spin current.

## Slide 9: Magnetic anisotropy
: Coercive field
: Volume
In-plane
Shape anisotropy
Perpendicular anisotropy
CoCrPt
Bulk
tCoFeB<1.3 nm
CoFeB
Mgo
Interface
B
H
Hk
z
y
Magnetization
x
30-80 KT at 300K
CoFeB
Ellipsoid
Notes: If volume increases then E barrier also increases, because of that spontaneous fluctuation minimizes.
id demagnetization factor
If volume increases then E barrier also increases, because of that spontaneous fluctuation minimizes.
𝑁_(𝑑−𝑦𝑦) id demagnetization factor

## Slide 10: 3D potential landscape of nanomagnet
Easy axis:
Magnet’s plane:
y
z
x
Hard axis:
Out of plane energy
barrier goes higher
Potential energy
Potential energy
x
y
z
Magnetization direction
φ

## Slide 11: Magnetic Field, H: Simplified 2D analysis
z
y
x
x
y
z
H is along
in-plane hard axis
Magnet’s plane:
x
y
z
Magnetization
direction
φ

## Slide 12: Potential Profiles H is along in-plane hard-axis
H
Hy in along of in-plane hard axis

## Slide 13: Potential profiles: H is along easy-axis
H
Hz in along easy axis

## Slide 14: Perpendicular anisotropy
Circular cross-section
HPMA
Easy axis:
Magnet’s plane:
Hard axis:
z
y
x
Energy barrier: 30-80 KT
(T=300 K)
Eshape ()
x
y
z
Magnetization
direction

## Slide 15: Perpendicular interface anisotropy
Ikeda, S. et al. "A perpendicular-anisotropy CoFeB–MgO magnetic tunnel junction."
Nature Materials 9 (2010) 721-724
Interfacial anisotropy
Bulk
MgO
Interface
z
y
x
CoFeB
In-plane
sample
Out-of-plane
sample

## Slide 16: Magnetization dynamics Landau-Lifshitz (LL) equation
precession
damping
M= Magnetization
E= Potential energy
=Volume
Performance metrics
Phenomenological
damping parameter
Switching delay and energy dissipation
Damping causes a transfer of energy from macroscopic motion to microscopic thermal motion, which results in internal energy losses
A damping parameter takes into account the rate of energy transfer
precession
Landau and Lifshitz, Phy. Z. Sowjet. 8, 101 (1935)

## Slide 17: Magnetization dynamics Landau-Lifshitz-Gilbert (LLG) equation
LL
damping
In standard form
LL cannot account for large damping in thin Permalloy sheets, adjusted by Gilbert
damping
LLG
LLG
LL
Gilbert, IEEE Trans. Magn. 40, 3443 (2004)
Notes: Landau and Lifshitz formulated the theory of dynamics of magnetization in ferromagnetic bodies

## Slide 18: Magnetization switching: Magnetic field
z
y
Hy
Hz
(b)
(a)
(c)
(d)
DOWN to UP
Magnetic Random Access Memory (MRAM)
Huge energy dissipation to generate the magnetic field KT (~1 pJ)
Magnetic field is difficult to confine in small space
Spin current
Voltage control
Notes: Why two magnetic field? If only one magnetic field Hz then we required high magnetic field and it may change neighbouring bit.

## Slide 19: Giant Magneto-Resistance (GMR)
A. Fert, M.N Baibich et al., Phys. Rev. Lett. 61, 2472 (1988)
P. Grunberg, G. Binash et al., Phys. Rev. B 39, 4828 (1989)
Giant Magneto-Resistance (GMR)
1988

## Slide 20: Tunneling magneto-resistance (TMR)
Conductance is proportional to the density of states
NL↑, NR↑, NL↓, NR↓
Julliere, M. Tunneling between ferromagnetic film. Phys. Lett. A 54, 225-226 (1975)
Moodera, J. S. et al., Phys. Rev. Lett. 74, 3273 (1995)
Mathon, J. et al., Phys. Rev. B 63, 220403 (2001), Butler, W. et al., Phys. Rev. B 63, 054416 (2001)
Yuasa, S. et al., Nature Mater. 3, 868 (2004), Parkin, S. et al., Nature Mater. 3, 862-867 (2004)
Reported 1975 (prior to GMR)
TMR>500% using MgO spacer
Insulator
e.g., Al2O3, MgO
Left (L)
Right (R)
Left (L)
Right (R)

## Slide 21: Spin-transfer-torque (STT)
A spin-polarized current transfers its spin angular momentum to the magnetic body
Ohmic dissipation
Current density: 107 A/cm2
Huge energy dissipation
Spin polarization
STT can rotate the magnetization axis of the nanomagnet
J. C. Slonczewski, J. Magn. Mater.159, L1 (1996)
L. Berger, Phy. Rev. B 54, 9353 (1996)
Slonczewski
Berger
Oliver E. Buckley Condensed Matter Physics Prize in 2013 “For predicting Spin-transfer torque ”
1998: Experimentally
demonstrated

## Slide 22: Switching nanomagnets with STT
20 nm (circular cross-section)
Current: ~10 μA
Energy dissipation: ~1fJ
Current passing through fixed magnet gets spin-polarized

## Slide 23: Spin Hall effect
Ordinary Hall effect
Hall voltage
NO
Spin accumulation
Anomalous Hall effect
Hall voltage
AND
Spin accumulation
(Pure) Spin Hall effect
NO Hall voltage
BUT
Spin accumulation
Hall voltage = 2
Spin accumulation = 0
Hall voltage = 1
Spin accumulation = 3
Hall voltage = 0
Spin accumulation = 2
Spin-orbit
interaction
Magnetic field
Magnetization
Pt, Ta,
W, CuBi
Magnets
Non-magnets
Non-magnets

## Slide 24: Spin-orbit-torque (SOT)
Material parameters
Charge
Spin
Jc
Dimension
Energy dissipation: ~0.1 fJ
Roy, K., J. Phys. D: Appl. Phys. (Fast Track Communication) 47 , 422001 (2014)
Pure spin current
Spin-orbit interaction
Pt, Ta, W, CuBi
Spin-Hall material
b

## Slide 25: Spin-transfer-torque (Direct SHE) and Spin pumping (Inverse SHE)
Charge current generates spin current via direct SHE
Spin current exerts spin-transfer-torque on magnet
Precessing magnet injects pure spin current
Spin current generates charge current via inverse SHE
Onsager’s reciprocity

## Slide 26: Ferromagnetic resonance with damping
FMR linewidth
Half width at half maximum (HWHM)
Derivative FMR spectra
precession
damping
Transverse AC field
Negative damping to keep the magnetization rotating
)
In-plane FMR
Perpendicular FMR

## Slide 27: Spin pumping
Tserkovnyak et al., Phys. Rev. Lett. 88, 117601 (2002); Rev. Mod. Phys. 77 , 1375 (2005)
Py
Py
Pt
Mosendz et al. Phys. Rev. B 82,
1214403 (2010)
An excited ferromagnet ejects spins into the adjacent materials
Increase in magnetization damping
Increase in linewidth
FMR linewidth

## Slide 28: Contents
Introduction
  Spintronics and nanomagnetics
  Magnetic anisotropy
  Magneto-resistance
  Magnetization dynamics
  Switching using magnetic field
  Spin-transfer-torque
  Spin Hall effect and spin-orbit-torque
  Ferromagnetic resonance and spin pumping
Plan of works
  Probing the resistivity of ultra-thin spin-orbit materials
  Spin-torque ferromagnetic resonance
  Switch magnetization using spin-orbit-torque
Experimental
  Electron beam lithography and scanning electron microscopy (SEM)
  Ferromagnetic resonance
  Vibrating sample magnetometer (VSM)
  X-Ray diffraction
  Electrical characterization using probe station and accessories
  Four-probe setup
  Signal generator, oscilloscope, spectrum analyser, bias-tee and power supply
  Atomic/Magnetic force microscopy (AFM/MFM)
  Sputtering

## Slide 29: Four-probe method
It allows to measure resistance excluding contact resistance
We need to measure the resistivity of spin-orbit layer
CoFeB
MgO
Notes: It allows to measure resistance excluding contact resistance, because unwanted voltage drop because of contact resistance is removed during measurement of voltage difference between B and C.
In four probe measurement, all probes contact with material of unknown resistance. A DC current is force between the outer two probe, and a voltmeter measure the voltage difference between the inner two probes. The resistivity is calculated from geometric factor, the source current and the voltage measurement.

## Slide 30: Spin-torque ferromagnetic resonance (ST-FMR)
30
Precessing
Magnetization
4
3
1
2
Spin Hall effect (SHE) layer
~
in -direction
Bias-Tee
6
5
In ST-FMR experiments, an alternating current in spin-orbit materials drives the magnetization precession in an adjacent magnet via direct spin Hall effect (SHE)
It pumps spins into the spin-orbit layer detected as a charge voltage/current via inverse spin Hall effect (ISHE)
RF signal generator, spectrum analyzer and electromagnet
Bias-Tee: Simultaneous application of AC and detection of DC
10 GHz
100 KHz

## Slide 31: Switching perpendicular magnets
van den Brink et al APL 104, 012403 (2014)
Difficult to create gradient experimentally
in small 10 nm dimensions
Passing perpendicular JSTT
Lateral asymmetry
Tilted anisotropy
Issue with scaling
Does not help much compared to ONLY using JSTT
Issue with switching perpendicular nanomagnets
Yu et al, Nature Nano 9, 548 (2014)
You et al, PNAS 112, 10310 (2015)
Magnetization can rotate only in direction
Free Layer
Insulator
Fixed Layer
Jc
Js

## Slide 32: Contents
Introduction
  Spintronics and nanomagnetics
  Magnetic anisotropy
  Magneto-resistance
  Magnetization dynamics
  Switching using magnetic field
  Spin-transfer-torque
  Spin Hall effect and spin-orbit-torque
  Ferromagnetic resonance and spin pumping
Plan of works
  Probing the resistivity of ultra-thin spin-orbit materials
  Spin-torque ferromagnetic resonance
  Switch magnetization using spin-orbit-torque
Experimental
  Electron beam lithography (EBL) and scanning electron microscopy (SEM)
  Ferromagnetic resonance (FMR)
  Vibrating sample magnetometer (VSM)
  Electrical characterization using probe station and accessories
  Four-probe setup
  Signal generator, oscilloscope, spectrum analyser, bias-tee and power supply
  X-Ray diffraction (XRD)
  Atomic/Magnetic force microscopy (AFM/MFM)
  Sputtering

## Slide 33: Scanning electron microscope (SEM)
It was developed due to the limitation of optical microscope
SEM is used to visualize the surface of an object
(a)
(b)
Illustration of resolution in (a) Airy disk and (b) wave front.
Field-emission electron gun
Notes: Scanning electron microscopes are scientific instruments that use a beam of energetic electrons to examine object on a very fine scale. SEM used to visualize the surface of an object. SEM was developed due to the limitation of Light Microscopes.
SEM uses a focused electron beam over a surface to create an image. The electrons interact with the atom that make up the sample producing signals that contain information about the sample’s surface topography, and different properties like composition of materials. SEM scan the surface of the specimen systematically, producing large number of signals. These electron signals are eventually converted to a visual signal displayed on a cathode ray tube (CRT). SEM is a type of electron microscope that images a sample by scanning it with a high energy beam of electron in a raster scan pattern.

## Slide 34: Working principle of SEM
The electrons interact with the atom that make up the sample producing signals that contain information about the sample
Electron source
Anode
Condenser lens
Objective lens
Scan coil
Sample
Secondary electron detector
Basic components of SEM
Backscatter electron detector
Notes: Electron microscopes are scientific instruments that use a beam of energetic electrons to examine object on a very fine scale. SEM used to visualize the surface of an object. SEM was developed due to the limitation of Light Microscopes.
SEM uses a focused electron beam over a surface to create an image. The electrons interact with the atom that make up the sample producing signals that contain information about the sample’s surface topography, and different properties like composition of materials. SEM scan the surface of the specimen systematically, producing large number of signals. These electron signals are eventually converted to a visual signal displayed on a cathode ray tube (CRT). SEM is a type of electron microscope that images a sample by scanning it with a high energy beam of electron in a raster scan pattern.

## Slide 35: Electronic beam lithography (EBL)
Resist layer
Substrate
Exposure with e-beam
Development
Metal deposition
Lift-off
Positive-resist: PMMA
For achieving 100 nm thickness:
0.9 ml PMMA for 2 inch wafer
At 500 RPM for 5 s for spreading and then 2100 RPM for 30 s
Pre bake: for 90 s
For development:
IPA+MIBK with 3:1 for 30 s
IPA for 30 s
Metal deposition: Sputtering
Lift-of: Acetone for 10 s in ultrasonic cleaner
Draw patterns
Notes: PMMA: Polymethyl methacrylate, IPA: Isopropyl alcohol

## Slide 36: EBL result
Gold standard 617 sample
Gold standard 617_3 sample
Different structures after EBL
Thickness measurement
in SEM
I have seen 5 nm gold structure in SEM
Measured thickness of resist layer
Draw the pattern in EBL software
Fabricated both draw pattern and standard pattern
100 nm
20 nm
200 nm
20 m
2 m
20 m

## Slide 37: Vibrating sample magnetometer (VSM)
Highly sensitive magnetic moment measurement device.
Magnetic field up to ~70k Oe (7 T)
Works on the basic principle of Faraday’s law
Sample rod
Adaptor
Sample
M
H
Co 5 nm sample
Notes: SQUID-VSM ( Superconducting Quantum Interface Device Vibrating Sample Magnetometer)

## Slide 38: Vibrating sample magnetometer (VSM)
For rotation,
rotate sample clockwise
For rotation,
rotate rod anticlockwise
In-plane samples
Energy
Out of plane energy
barrier goes higher
x
z
M
y
H
E(,)
Rotate from the top
z
x
y
M
H
x
y
z
M
H
x
y
z
H
M
x
y
z
H
M
Notes: Magnitude of a circulation of electric field around a closed loop is equal to the rate of change of the magnetic flux through the are enclosed by the loop.

## Slide 39: Vibrating sample magnetometer (VSM)
For rotation, tilt the sample by using glass pieces
For rotation,
rotate sample
Out-of-plane samples
y
z
x
M
H
z
y
x
M
H
Energy
Out of plane energy
barrier goes higher
z
x
y
H
z
x
M
y
H
E(,)
x
y
z
H
M
x
y
H
M
z
Notes: Magnitude of a circulation of electric field around a closed loop is equal to the rate of change of the magnetic flux through the are enclosed by the loop.

## Slide 40: Ferromagnetic resonance (FMR)
In-plane samples
Energy
Out of plane energy
barrier goes higher
For rotation, rotate sample anti-clockwise
y
x
z
M
H
x
M
z
H
y
x
z
y
M
H
For rotation, rotate rod in anticlockwise
H
M
y
z
x
x
y
z
M
H
E(,)
Rotate from the top
Notes: Magnitude of a circulation of electric field around a closed loop is equal to the rate of change of the magnetic flux through the are enclosed by the loop.

## Slide 41: Ferromagnetic resonance (FMR)
Out-of-plane samples
Energy
Out of plane energy
barrier goes higher
z
y
x
H
H
M
x
y
z
H
M
For rotation, tilt the sample by using glass pieces
z
y
x
M
For rotation,
rotate sample
H
M
y
x
z
H
E(,)
Notes: Magnitude of a circulation of electric field around a closed loop is equal to the rate of change of the magnetic flux through the are enclosed by the loop.

## Slide 42
Thank you

## Slide 43: I have done
Wafer cleaning, cutting and trimming
Spin coating (achieved 100 nm thickness)
Measured the sample thickness in SEM
Electron beam lithography
Imaging in SEM and TEM
EDX
Magnetize sample by using Electromagnet
Vibrating sample magnetometer (VSM)
Ferromagnetic resonance on hard disc sample
Anneal the sample at high temperature
Measure electrical characteristics by using probe station
Making waveguide for ST-FRM setup
Generate signal from signal generator and record waveforms on spectrum analyzer.

## Slide 44: LL and LLG

## Slide 45: FMR

## Slide 46: FMR

## Slide 47: FMR

## Slide 48: FMR

## Slide 49: FMR

## Slide 50: FMR
FMR linewidth
Half width at half maximum (HWHM)
Derivative FMR spectra

## Slide 51: SAF: Interlayer exchange coupling
SAF: Synthetic antiferromagnetic layer

## Slide 52: Four-probe method
Schmiedl, E et al. (2008). The electrical resistivity of ultra-thin copper films. Zeitschrift für Naturforschung A, 63(10-11), 739-744.
(◦) Experimental data
(-) statistical model
(- --) Basis of fit parameters
For equal spacing
For unequal spacing
Notes: In four probe measurement, all probes contact with material of unknown resistance. A DC current is force between the outer two probe, and a voltmeter measure the voltage difference between the inner two probes. The resistivity is calculated from geometric factor, the source current and the voltage measurement.

## Slide 53: ST-FMR setup
Signal generator
Bias-Tee
Oscilloscope
Waveguide and
gauss probe
Spectrum-analyzer waveform
Electromagnet

## Slide 54: Single-domain and Multi-domain

## Slide 55: Depth of field
Depth of focus: The portion of the image that appears acceptably in focus is called the depth of focus.
Working distance: Distance from the final pole piece of the lens to the sample when the image is in focus.
Depth of field at different working distance
Different electrons

## Slide 56: Contents
Introduction
  Spintronics and nanomagnetics
  Magnetic anisotropy
  Magneto-resistance
  Magnetization dynamics
  Switching using magnetic field
  Spin-transfer-torque
  Spin Hall effect and spin-orbit-torque
  Ferromagnetic resonance and spin pumping
Plan of works
  Probing the resistivity of ultra-thin spin-orbit materials
  Spin-torque ferromagnetic resonance
  Switch magnetization using spin-orbit-torque
Experimental
  Electron beam lithography (EBL) and scanning electron microscope (SEM)
  Ferromagnetic resonance (FMR)
  Vibrating sample magnetometer (VSM)
  X-Ray diffraction (XRD)
  Transmission electron microscope (TEM)
  Atomic/Magnetic force microscope (AFM/MFM)
  Sputtering
  Electrical characterization using probe station and accessories
  Four-probe setup
  Signal generator, oscilloscope, spectrum analyser, bias-tee and power supply

## Slide 57: Hy vs θmin
Hy in along of in-plane hard axis

## Slide 58: Spin-transfer-torque (Direct SHE) and Spin pumping (Inverse SHE)
Charge current generates spin current via direct SHE
Spin current exerts spin-transfer-torque on magnet
Precessing magnet injects pure spin current
Spin current generates charge current via inverse SHE
Onsager’s reciprocity