## Slide 1: Energy-Efficient Neuromorphic Computing
Khritish Kumar Behera 17125
Mail: khritish17@iiserb.ac.in
Indian Institute of Science Education and Research [IISER] Bhopal
Advisor: Dr. Kuntal Roy
Mail: kuntal@iiserb.ac.in
MS Project: End Term Presentation
Date: 23-11-2021

## Slide 2: Content
Recap
Motivation
Artificial neural network
Character recognition model
Neural Network using spintronics
Magnetic anisotropy
Magnetic Field applied along in-plane easy and hard axis
Multiferroics and Multiferroic composite
Magnetostriction
Proposed device
Experimental
Results after Magnetic Thermal Annealing
Piezoelectric Simulation with multiple inputs
Instruments learned
LabView measurement automation
Future Plans

## Slide 3: Neuromorphic Computing
Neuromorphic Computing ?
Mimicking brains computation process
Why?
Computers, faster than brain
Distinct capabilities of brain
  Face recognition in crowd
  Low energy consumption
AI algorithms, were developed
  Runs on transistor-based devices
Power Hungry
MegatronLM, Nvidia’s NLP model
  9 days training, costs 27,684 kWh[1]
1: https://searchenterpriseai.techtarget.com/feature/Energy-consumption-of-AI-poses-environmental-problems
Piezoelectric
Magnetostrictive
Insulator
TMR
Non-Boolean Computation

## Slide 4: Artificial Neural Network (ANN)
b
System of interconnected neurons
Neuron
Components of a neuron
Multiple inputs
Weights and bias
Summation block
Activation block
Architecture
Output of a neuron, connected to all other neurons in the next layer
Three layers: Input, Hidden and Output layer

## Slide 5: ANN: Sequential Process and Optimizing Parameter
b
b
Summation
Activation
Non-linear function
Optimizing parameter: Weights and Biases
Weight
b
Bias
Strength of the edges
Sets the activation function

## Slide 6: ANN: Two Phase Process
Training
Evaluation
X
O
Error: T - O
Training Data: (X , T)
X: Input
T: Output for X
Weights and Biases are constructed
NN learns the underlying feature
After the model is properly trained
Inputs with pre-unknown output is fed
Y
O
Evaluation Data: (Y , ?)
Y: Input

## Slide 7: Character Recognition Model
7x5 pixel values character recognition model predicts character
Noisy/Perturbed data
Predicted data
Character recognition model

## Slide 8: Spintronics: Spin-Electronics
Electron
Spin
Spin
UP
DOWN
Bits
1
0
Spintronic devices, advantages over transistor
  non-volatile
  endurable
Transistor, requires extra circuitry
There are no charge movement, only spin rotation
  No ohmic , dissipation
  Dissipation due to magnetization damping
  Dissipation due to applied external charge voltage/current
Electron Beam Lithography

## Slide 9: Magnetic Anisotropy
CoFeB
Ellipsoid
Sphere
Elliptical Cylinder
In-plane Shape anisotropy
No anisotropy
Difficult to fabricate
z
y
Magnetization
x
Volume
Coercive field
M
H
Hk
30-80 KT at 300 K

## Slide 10: Magnetic Field applied along in-plane hard axis
y
z
x
x
z
y
Magnetic Field, along Y-axis

## Slide 11: Magnetic Filed applied along in-plane easy axis
y
z
x
x
z
y
Magnetic Field, along Z-axis

## Slide 12: Perpendicular Anisotropy
CoCrPt
Bulk
tCoFeB<1.3 nm
CoFeB
MgO
Interface
Priyesh Kumar
IISER Bhopal
Circular cross-section
HPMA
Easy axis:
Magnet’s plane:
Hard axis:
z
y
x
x
y
z
Magnetization
direction
12

## Slide 13: Multiferroics and Multiferroic Composites
P
E
H
M
Piezoelectricity
Magnetostriction
Magnetoelectricity (intrinsic)
Multiferroics
  Room-temperature operation
  Weak magnetoelectric coupling
Piezoelectric
Strain
Magnetostrictive
Multiferroic Composite

## Slide 14: Magnetostriction
Magnetostrictive Materials: Certain ferromagnetic specimen changes its shape (strain:) during the process of magnetization
Magnetostriction Co-efficient
Magnetic Anisotropy
Stress Anisotropy
Cobalt:
FeGa:

## Slide 15: Multiferroic composites Voltage vs stress anisotropy
Y: Young’s modulus
strain transfer
Magnetostrictive layer
with high
Choose piezoelectric layer with high de-coefficient
Stress Anisotropy (for FeGa):
(max.)
Vin
tpiezo
Piezoelectric
Magnetostrictive

## Slide 16: Proposed Device
Magnetostrictive
Insulator
Write
ReadMTJ
Piezoelectric
.
.
x1
x2
xn
Electric Potential to Piezoelectric
Stress anisotropy in Piezoelectric
Stress anisotropy in Magnetostrictive
Magnetic anisotropy in Magnetostrictive
Magnetization direction changes in TMR
Generation of variable resistance
X
Y

## Slide 17: Magnetic Thermal Annealing (MTA)
Lattice and shape deformities in material degrade its quality
Removing this anomalies high quality, high performance
Thermal Annealing
Raising, maintaining, slowly reducing its temperature
Time
Temperature
Atoms, diffuse more easily to their proper location
Maintaining high temperature, achieves equilibrium, and removes structural imperfection
Effects of thermal annealing
Magnetic Thermal Annealing
External magnetic field applied during thermal annealing

## Slide 18: Magnetic Thermal Annealing (MTA)
Effects of magnetic thermal annealing
Reorients the easy axis of ferromagnetic materials or axis of spontaneous magnetization vector
Easy axis
If lattice has more deformities may not be any major global symmetry Magnetization will be weekend
If a lattice shows specific symmetry easy axis will normally reflect the symmetry
Deformed Ferromagnetic material, annealed at high temperature
Spins of individual atom will align along the external applied field
When the temperature is reduced the material attains a new magnetization direction

## Slide 19: Magnetic Thermal Annealing (MTA)
Electromagnet
CCPS
Heater
Pirani Gauge
Vacuum Pump
Chiller
Heater
MTA setup
Heating chamber
Heater PID
Vacuum pipe
Vacuum pipe
EM poles

## Slide 20: Experimental results after magnetic thermal annealing
Before MTA
After MTA
22 times more M-H area
At for 1 Hr.

## Slide 21: Small Instruments
Hot Plate
Ceramic hotplate
Mode selection buttons
Start/Stop buttons
Ultrasonic Cleaner
Mode selection buttons
Start/Stop buttons
Spin Coater
Nylon Bowl
LCD display & Keyboard
Chuck
Shaker
Adjustable rollers
RPM and time controllers

## Slide 22: Small Instruments
Nitrogen Gun and Nitrogen Cylinder
Hot Air Oven
ON/OFF button
PID controller
Heater indicators
Gas cylinder
Air gun
Heater indicator
RPM controller
Nylon chamber
PID controller
Rota Mantle
Pipes to transport

## Slide 23: Small Instruments
Toxic vapors or fumes prevention
Spill containment
Fume Hood
Vacuum Desiccator
Vacuum pump
Desiccator
Desiccator Knob
Muffle Furnace
PID controller
Heater indicator
Heating chamber
Energy regulator

## Slide 24: Small Instruments
Source Meter
Power Supply
I
III
IV
II
I
III
Delivers power to the load
Dissipate
power
Delivers power to the load

## Slide 25: Small Instruments
Probe Station
Oscilloscope
Microscope
Display
Input channel
Settings
Diode IV characteristics
Micro-positioner
Light source
Chuck
Camera
SMU and Power Supply can be connected to the probe station

## Slide 26: Automation in measurement: LabView
LabView
Graphical programming environment
For, automated research, validation, and production test systems
Control and synchronize different devices from different companies
Centralized system for data acquisition
Flexibility in programming the devices

## Slide 27: Power Supply measurement automation
Programming power supply as a stepper and sweep

## Slide 28: Power Supply measurement automation
1kResistor
Diode
MOS S170

## Slide 29: Source Measuring Unit automation
Programming SMU as sweep

## Slide 30: Source Measuring Unit automation
1kResistor
Diode
MOS S170

## Slide 31: Future Plans
 | TASK | ECS501 |  | ECS502 | 
 |  | MID-TERM | END-TERM | MID-TERM | END TERM
1 | Character recognition implementation |  |  |  | 
2 | Magnetic thermal annealing |  |  |  | 
3 | Different experimental apparatus |  |  |  | 
4 | LabView for automation of different devices |  |  |  | 
5 | Piezoelectric |  |  |  | 
6 | Sputtering |  |  |  | 
7 | Electron beam lithography |  |  |  | 
8 | Block co-polymer lithography |  |  |  | 

## Slide 32
?
Thank You

## Slide 33: Magnetic Thermal Annealing (MTA)
When the temperature is reduced, the lattice becomes locked or frozen
Material attains new magnetization direction
Magnetic thermal annealing
Reorients the easy axis
Removes lattice defects
Removes shape deformities

## Slide 34: Perpendicular Anisotropy
Ikeda, S. et al. "A perpendicular-anisotropy CoFeB–MgO magnetic tunnel junction."
Nature Materials 9 (2010) 721-724
Interfacial anisotropy
Bulk
MgO
Interface
z
y
x
CoFeB
In-plane
sample
Out-of-plane
sample

## Slide 35: Plan

## Slide 36: VSM (Vibrating Sample Magntometer)
SQUID converts current into voltage
Precise measurement depends on better sample centering
B field
SQUID with electronics
Flux transformer
Detection coil (or) Gradiometer
Sample position
Highly sensitive magnetic moment measure device over a range of (1.8 - 400 K) and (7 T)
Sample magnetic field cuts the winding and detects the gradient in terms of current
Flux transformer boost the flux
Works on basic principle
Of Faraday’s law

## Slide 37: BACKUP SLIDES

## Slide 38: Content
Character Recognition 7x5
Experimental Apparatus
Experiment results after magnetic thermal annealing
Piezoelectric simulation with multiple inputs
Explanation on magnetic parts
BCP Lithography
Atomic Force Microscopy (Piezo and magnetic response)
Spintronics more general understanding
Learn measurement apparatus and LabView

## Slide 39: Future Plans
 | TASK | ECS501 |  | ECS502 | 
 |  | MID-TERM | END-TERM | MID-TERM | END TERM
1 | Character Recognition Implementation |  |  |  | 
2 | Magnetic Thermal Annealing, Different experimental apparatus, LabView for automation of different devices |  |  |  | 
3 | Block Co-Polymer Lithography, |  |  |  | 

## Slide 40
Giant Magneto-Resistance (GMR)
A. Fert, M.N Baibich et al., Phys. Rev. Lett. 61, 2472 (1988)
P. Grunberg, G. Binash et al., Phys. Rev. B 39, 4828 (1989)
Giant Magneto-Resistance (GMR)
1988

## Slide 41
Tunneling Magneto-Resistance (TMR)
Conductance is proportional to the density of states
NL↑, NR↑, NL↓, NR↓
Julliere, M. Tunneling between ferromagnetic film. Phys. Lett. A 54, 225-226 (1975)
Moodera, J. S. et al., Phys. Rev. Lett. 74, 3273 (1995)
Mathon, J. et al., Phys. Rev. B 63, 220403 (2001), Butler, W. et al., Phys. Rev. B 63, 054416 (2001)
Yuasa, S. et al., Nature Mater. 3, 868 (2004), Parkin, S. et al., Nature Mater. 3, 862-867 (2004)
Reported 1975 (prior to GMR)
TMR>500% using MgO spacer
Insulator
e.g., Al2O3, MgO
Left (L)
Right (R)
Left (L)
Right (R)

## Slide 42: Experimental Instruments: Spin Coater
Nylon Bowl
LCD display & Keyboard
Chuck
Spreading thin films on flat substrate by centrifugal force
Substrate
Solvent Solution
Uniform Thin film is formed

## Slide 43: Experimental Instrument: Gaussmeter
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
I
I
B
Gaussmeter
Gauss Probe
Hall Effect
Gaussmeter is a static electronic magnetic field measurement device
Probes used in Gaussmeter:
Axial Probe: Measures the magnetic field parallel to the probe
Transversal Probe: Measures the magnetic field perpendicular to the probe

## Slide 44: Piezoelectric Simulation with multiple inputs

## Slide 45: Experimental Instrument: Probe Station
Probe Station is used to find the electrical characterization of a sample
Wafer is placed on the chuck
Microscope to view the sample
Micro-positioner to contact the sample
Micro-positioner is connected to the SMU or power supply, for stimulus

## Slide 46: Experimental Instrument: Source Meter
Keithley 2450
SMU can operate in four quadrants
  Quadrant I and III are sourcing
    I and V, same polarity
    Delivers power to the load
  Quadrant II and IV are sinking
    I and V, different polarity
    Dissipates power
Single Channel
Voltage Range: 20mV to 200V
Current Range: 10nA to 1A

## Slide 47: Experimental Instrument: Power Supply
Rohde & Schwarz NGL202
Similar to SMU, Power Supply operates in four quadrants
Two Channel device, equivalent to two SMU
High precision source and sink
Output Voltage per channel, 0 to 20V
Max. output current per channel
  For output vol., 6A
  For output vol., 3A
Notes: Power Supply is 2 quadrant, I and III

## Slide 48: Experimental Instrument: Electromagnet
Constant Current
Power Supply
Magnetic Coil
Gauss Probe
Chiller
Magnetic Coil: When electric current is passed through the magnetic coils it generates a constant magnetic field
Gauss Probe: It is used to measure the magnetic field generated between the poles
Constant Current Power Supply: Provides a constant current to the magnetic coil
Chiller: Is required to reduces the temperature of the magnetic coil
Notes: Put the big picture

## Slide 49: Experimental Instrument: Magnetic Thermal Annealing
Reorients the spin direction in the direction of the magnetic field, and passivates the dangling bond
Enhances the magnetic property of magnetic materials
Heater
Vacuum Pump
Heating of the sample is done in vacuum and the material MTA is made up of is not affected by the magnetic field
Magnetic Thermal Annealing Setup
Notes: Take the big complete picture and use arrows to point out

## Slide 50: Power Supply measurement automation

## Slide 51: Source Measuring Unit automation

## Slide 52: Block Co-Polymer Lithography
Sub 10nm lithography
Directed self-assembly
Bottom up approach

## Slide 53: EB Lithography

## Slide 54: New Contents
All experimental apparatus learned
Experimental results of Magnetic Thermal Annealing
Lab View
BCP Lithography
Electron Beam Lithography
Piezoelectric simulation for multiple inputs

## Slide 55: Experimental Slides
Oscilloscope
VSM slides
VI Characteristics of diode, resistance, transistor
Bar-magnet curve

## Slide 57: ANN: Activation Function
Inspired from biological neuron
Neurons won’t fire until a threshold is reached
Activation Function
Threshold is set by the bias term

## Slide 58: Content
Motivation Slide
Spintronics
Magnetic Anisotropy
Magnetic Field
Experiment results after magnetic thermal annealing
Piezoelectric simulation with multiple inputs
Explanation on magnetic parts
BCP Lithography
Atomic Force Microscopy (Piezo and magnetic response)
Spintronics more general understanding
Learn measurement apparatus and LabView

## Slide 59: Magnetic Field applied along in-plane hard axis
y
z
x
x
z
y
Magnetic Field, along Y-axis

## Slide 60: Magnetic Filed applied along in-plane easy axis
y
z
x
x
z
y
Magnetic Field, along Z-axis