## Slide 1
Energy-efficient ultra-sensitive magnetoelectric sensors for magnetocardiography and magnetoencephalography
JRF to SRF
M. Mohanlal Naik
Roll: 1910704, Email: mnaik19@iiserb.ac.in
Electrical Engineering and Computer Science (EECS) Dept.
Indian Institute of Science Education and Research (IISER) Bhopal
Advisor: Dr. Kuntal Roy, Email: kuntal@iiserb.ac.in
23-Oct-2021

## Slide 2: Contents
Motivation
Introduction
  Human brain
  Examples of Neuromagnetic fields
  Neural basis of magnetoencephalography
  Neural generation of electromagnetic fields
  Forward and inverse problems
  Instrumentation for magnetoencephalography
Ultrasensitive multiferroic sensor
  Interfacial perpendicular anisotropy between oxide and ferromagnet
  Demonstration of ultrasensitive piezoelectric-magnetostrictive sensors
  Instruments
  Sputtering
  Vibrating sample magnetometer
  Stress and strain machine
  Electromagnet
  Ultrasensitive measurement instruments

## Slide 3: Motivation: Ultrasensitive sensors
Seizure detection
Aging technologies
M. Hamalainen et al,
Rev. Mod. Phys. 65, 413 (1993)
Detectable signal at room-temperature is a challenge
Noise-cancellation techniques
Non-invasive studies of human brain
Ultrasensitive magnetic sensors
Magnetocardiography (MCG) Magnetoencephalography (MEG)
Magnetic Field Sensing
femto-Tesla
Multiferroic nanostructures
Voltage
Piezoelectric
Strain
Magnetostrictive
Piezoelectric characterization
  COMSOL modeling
  Material/Stress testing
  Strain gauge
Interfacial anisotropy characterization
Noise-cancellation techniques
  Differential amplifiers
Notes: Sensor is a transducer, it convert the magnetic field energy into electric field energy
For piezoelectric characterization we have to use COMSOL and characterize stress and strain
MEG –Femto tesla
MCG- pico tesla

## Slide 4: Introduction
P (or) N  +/- Electric potential from EEG
100  Time period of signal in milli second
m  Magnetic field
Electric potential
Magnetic field
First measurement of magnetic field of a human brain was captured by David Cohen (Cohen, 1972) from MIT
Magnetic field of an auditory response, measured by MEG
Notes: Each circle has same potential

## Slide 5: Current dipole
Point charge is a charge located in single point in space

## Slide 6: Limitations of current technology (SQUID)
Superconducting quantum interference device (SQUID)
People suffering from unconscious (coma) due to brain injury
Active brain of unconscious people fail to communicate to the world
Sensors to observe the active brain
  Magnetoencephalography (MEG)
  Electroencephalography (EEG)
Size is big and operating cost is high
Need cold environment like helium chamber (about 4 kelvin) with superconductors
Need magnetic shielded room to minimize external noise
Minimum duration of MEG-EEG recording sessions is about 30 min
MEG device with shielded room
SQUID working principle ?

## Slide 7: Working principle of SQUID
Negligible resistance at less than critical temperature
Perfect dia magnetic
Internal magnetic flux is quantized
Flux transform in super conductive material

## Slide 8
Non invasive MEG and EEG measure signals from the same synchronized neural activity in the brain
Electroencephalography (EEG): Capture electrical potential difference b/w two locations on scalps
Magnetoencephalography (MEG): Measure neuromagnetic signals from the brain
Electrocardiography (ECG): Non invasive device, helps to measure electric potential around the heart
Magnetocardiography (MCG): Instead of brain, heart is being measured
Heart magnetic fields are 5000 times greater than brain
Diagnose and monitor conditions affecting the heart
Biomedical instruments
This are techniques

## Slide 9: Neural basis of magnetoencephalography
Neuron
Cell body (Soma)
MEG concentrates on cerebral cortex (present on top layer of brain): 2-4 mm thick and 2500 cm2
Improve presentation
Notes: Generally we have two hemisphere and four in our brain,
Two hemisphere separated by longitudinal fissure and communicate by carpus callosum (group of neurons)
Four lobes separated by particular fissure and communicate by the neuron, which have the connection between white matter() and grey matter(occupied by the neurons )
____
This is the neuron with axon and this is the cell body
They are lot of other neuron cells connected to the cell body and shown cell signal receiver called dendrites
Electrical voltages generated in the neuron by the chemical gradient

## Slide 10: Neurons
Dendrites: Receive the stimuli
Soma (Neuron body): Contains genetic material in the form of chromosomes
Axon: Long fiber that carries the nerve impulses
Glial cell: Glue around neuron, helps to maintain proper concentration of ions
Oligodendrocytes: Acts as a insulating myelin sheath around neuron, helps to speeding signal transmission in central nervous system
Transfers information as electrical signals, by excitable tissues (Na+, K+ and Cl-)
At least 1010 neurons and 1014 synapses/interconnections in cerebral cortex

## Slide 11: Biological neuron vs Artificial neuron
Dendrites
Soma
(Neuron body)
Axon
.
.
.
Input
Summation & Activation function
Output
Biological neuron
Artificial neuron
Dendrites

## Slide 12: Ion mechanisms
Permeabilities
Concentration in milli mole/liter
Goldman's (1943), membrane potential equation
5 K+
140 K+
20 Cl-
120 Cl-
140
Na+
20 Na+
Direction of propagation
Volume current
Ohmic current
Current = 1 e-6 A, Radius = 100 e-6 m
Volume and ohmic currents
How concentration gradient is maintained
Get clarity on membrane
Barrier vs well
Why – in potential
Understand current and radius
Calculation of current ?
Diffusion current equation
How the signal propagate in particular direction
Notes: Goldman derived an voltage equation, on ion diffusion through the membrane. At equilibrium membrane potential of -70 mV, Na+ and Cl- has higher concentration on extra cellular membrane, where as in case of K+, concentration is higher in intra cellular membrane. the permeability will change with ion diffusion through the channels.

## Slide 14: Electrical potential in the neuron
Releasing transmitter molecules
Change in permeability
Change in membrane potential
Excitatory synapse
Inhibitory synapse
Concise slide on signal propagation
Depolarization
+
Inflow Na+ ends
Outflow K+ dominates
Na+ inflow begins
Repolarization
-
Sufficiently depolarized postsynaptic neurons cause action potential

## Slide 15: Equivalent current dipole
Tangential dipole are magnetically active but electrically silent
Current dipole is an equivalent source of electric field and magnetic fields
Radial dipole are electrically active but magnetically silent
T
R
Simultaneous and synchronous active group of neurons create equivalent current dipole
Why magnetically can’t the radial dipole
Notes: Theoretically prediction is that --> Radial dipole cant produce the magnetic field out of spherical shell but practically our head is not spherical in shape

## Slide 16: Neural generation of electromagnetic field
Maxwell’s equations and continuity equation help
to calculate the E and B of the brain tissue
when conductivity and electric current are known
Characteristic length>> Radius of head
Quasistatic approximation to be valid
Still we can calculate

Understand input and output of the model
Understand cross product and dot product

## Slide 17: Neural generation of electromagnetic field

( )

Maxwell’s equations and continuity equation help
to calculate the E and B of the brain tissue
when conductivity and electric current are known
Notes: Get about what is input and output

## Slide 18: Forward/Inverse problem
Condu-ctivity
E (or) V
B
Current dipole
E (or) V B
Calculating the magnetic field and electric field from known primary current and conductivity distribution of head
Inverse problem is estimating the current source (Dipole) with help of measured distribution of magnetic field
Primary current distribution from either B=0, E=0 or both
Prepare the slide better

## Slide 19: Forward problem
Calculate magnetic field outside the head from primary current distribution in the brain
From Biot-Savart Law, magnetic field generated by neuron primary current
From quasistatic approximation

## Slide 20: Inverse problem
Estimating the cerebral current source underlaying a measured distribution of the magnetic field
The current distribution inside a conductor cannot be retrieved uniquely from the knowledge of electromagnetic field outside (Helmholtz 1853)
Primary current distributions are
    Magnetically silent (B=0 outside conductor), spherically symmetric conductor/radial dipole
    Electrically silent (E=0 outside conductor), current loop
    Both
Update the slide
Understand the slide
Notes: Add equations

## Slide 21: Gradiometer
Noise cancellation of external field can be done by using same coil cross section area with oppositely oriented winding
A simple wire loop is a magnetometer
Gradiometer has compensation coil (upper) and pickup coil (lower)
Pickup coil captures field from source
24 channel 12-2 gradiometer was developed in Helsinki university
Nano Ampere range
Understand the x and y axis
Notes: In steady magnetic field gradiometer produce zero current (Gradiometer are opposition)
Variable magnetic field produce net current in gradiometer

## Slide 22: Noise cancellation
Far reference sensor (noise)
Near source sensor (source field)
Output voltage of an amplifier
Differential mode differential amplifier
Common mode differential amplifier
Op-amp

## Slide 23: Contents
Motivation
Introduction
  Human brain
  Examples of Neuromagnetic fields
  Neural basis of magnetoencephalography
  Neural generation of electromagnetic fields
  Forward and inverse problems
  Instrumentation for magnetoencephalography
Ultrasensitive multiferroic sensor
  Interfacial perpendicular anisotropy between oxide and ferromagnet
  Demonstration of ultrasensitive piezoelectric-magnetostrictive sensors
  Instruments
  Sputtering
  Vibrating sample magnetometer
  Stress and strain machine
  Electromagnet
  Ultrasensitive measurement instruments

## Slide 24: Multiferroic materials and composites
E
P
H
M
E, H
P, M
Ferroelectric
Ferromagnetic
Multiferroic
and magnetoelectric
Multiferroic composites
Piezoelectric
Strain
Magnetostrictive
Terfenol-D, FeGa
PZN-PT, PMN-PT
Multiferroic materials
Multiferroic
BiFeO3
3500 Oe  6 kV/cm, PZN-PT/Terfenol-D
Liu, M. et al., J. Appl. Phys. 112, 063917 (2012)
Notes: lead zinc niobate-lead titanate (PZN-PT), lead magnesium niobate-lead titanate (PMN-PT)

## Slide 25: Multiferroic materials
P
E
H
M
Piezoelectricity
Magnetostriction
Magnetoelectricity (intrinsic)
Multiferroic materials can have intrinsic magnetoelectric coupling
  Room-temperature operation
  Not enough magnetoelectric coupling
Issues for
technological applications
Problems at room temperature
Notes: Here, E H and sigma are electric field, magnetic field and stress, respectively and they can be applied externally
P M and epsilon are polarization, magnetization and strain, which are macroscopic observables
Here they can be intrinsic coupling between E and H but there are issue for technological applications

## Slide 26: Multiferroic composites
Multiferroic heterostructures
Stress-mediated
P
E
H
M
Piezoelectricity
Magnetostriction
Magnetoelectricity (intrinsic)
Enhanced magnetoelectric
coupling by strain
Piezoelectric
Strain
Magnetostrictive

## Slide 27: Magnetostriction
Magnetostrictive Material : Certain ferromagnetic specimen changes its shape (strain:) during the process of magnetization
Magnetostrictive Anisotropy ↔ Stress Anisotropy
Magnetostriction Co-efficient
Cobalt:
FeGa:

## Slide 28: Multiferroic composites Voltage vs stress anisotropy
Vin
tpiezo
Y: Young’s modulus
strain transfer
Piezoelectric
Magnetostrictive
Magnetostrictive layer
with high
Choose piezoelectric layer with high de-coefficient
Stress Anisotropy (for FeGa):
(max.)

## Slide 29: Magnetic anisotropy
In-plane shape anisotropy
(degree)
θ (degree)
Potential energy
MgO(0.8nm)
CoFeB
tCoFeB < 1.3 nm
Perpendicular anisotropy
Bulk
Interface
CoCrPt (6nm)
Notes: Iron, Cobalt. Nickel
CrCoPt (6nm)
Magnetic anisotropy: The energy of a magnetic material is different in different direction(?)

## Slide 30: Potential landscape of in-plane anisotropy
Z-axis
Y-axis
X-axis
Out of plane energy barrier
goes higher at
x-axis
y-axis
z-axis
Potential energy
(degree)
θ (degree)
= + +
(?)
Focus on yellow text box

## Slide 31: Perpendicular anisotropy
Z-axis
Y-axis
X-axis
x-axis
y-axis
z-axis
Notes: 1. Change figure

## Slide 32: Hy vs θmin
Applied field along hard axis (y-axis)
Applied field along easy axis (z-axis)
x-axis
y-axis
z-axis
,
Easy axis and hard axis make separate slides
Z-axis
Y-axis
X-axis
Notes: Easy axis applied magnetic field at theta = 0 degrees
Hard axis applied magnetic field at theta = 90 degrees

## Slide 33: Applied magnetic field along easy axis
x-axis
y-axis
z-axis
Easy axis and hard axis make separate slides
Z-axis
Y-axis
X-axis
Applied field along easy axis (z-axis)
Notes: Easy axis applied magnetic field at theta = 0 degrees
Hard axis applied magnetic field at theta = 90 degrees

## Slide 34: Applied magnetic field along hard axis
x-axis
y-axis
z-axis
Easy axis and hard axis make separate slides
Z-axis
Y-axis
X-axis
Applied field along hard axis (y-axis)
Notes: Easy axis applied magnetic field at theta = 0 degrees
Hard axis applied magnetic field at theta = 90 degrees

## Slide 35: Interfacial perpendicular anisotropy between oxide and ferromagnet
Perpendicular anisotropy : Easy axes
is perpendicular to the sample surface and hard axis is in-plane of the sample
S.Ikeda et al, Nature Vol 9, DOI:10.1038/NMAT2804 (2010)
MgO
CoFeB
tCoFeB < 1.3 nm
Interfacial anisotropy
Bulk
Interface
Notes: In plane magnetic field is creating an hystersis Easy axis
No hysteresis  Hard axis (Magnetic field is saturating)
Interface of piezoelectric
Paper name
Explain the linear curve

## Slide 36: Contents
Motivation
Introduction
  Human brain
  Examples of Neuromagnetic fields
  Neural basis of magnetoencephalography
  Neural generation of electromagnetic fields
  Forward and inverse problems
  Instrumentation for magnetoencephalography
Ultrasensitive multiferroic sensor
  Interfacial perpendicular anisotropy between oxide and ferromagnet
  Demonstration of ultrasensitive piezoelectric-magnetostrictive sensors
  Instruments
  Sputtering
  Vibrating sample magnetometer
  Stress and strain machine
  Electromagnet
  Ultrasensitive measurement instruments

## Slide 37: Experimental
Sputtering
Vibrating sample magnetometer
Stress and strain machine
Electromagnet
Magnetic thermal annealing
Ultrasensitive measurement instruments
Magnetic force microscopy
Update the slide

## Slide 38: Sputtering
Sputtering is a technique to deposit metals/Insulators on a substrate
Magnetron sputtering : Magnet keeps high density of sputtering ions, leads higher efficiency
DC - Metal deposition
RF - Insulator deposition
Argon gas
Vacuum pump
v
Chamber pressure
10e-9 mbar with turbo pump
Cathodic sputtering : Inelastic collision between Ar+ ions and target atoms
High vacuum allows
sufficient mean free path
Notes: Energies are different with same momentum

## Slide 39: Sputtering
Sputtering is a technique to deposit metals/Insulators on a substrate
Magnetron sputtering
Magnet keeps high density of sputtering ions, leads higher efficiency
Inelastic collision between Ar+ ions and target atoms
DC - Metal deposition
RF - Insulator deposition
Chamber pressure
10e-9 mbar with turbo pump
Magnetron sputtering
High vacuum leads sufficient mean free path
Targets
Sputtering
Notes: Energies are different with same momentum

## Slide 40: Sputtering
Sputtering is the process of atoms of a material are ejected from a target by the bombardment of high-energy particles
Ions of sufficient energy must be created and directed towards the surface of a target to eject atoms from the material
Ejected atoms must he able to move freely towards the object to be coated
Why sputter coating with low pressures
To maintain high ion energies
To prevent too many atom-gas collisions after ejection from the target
Sputter coating with high pressures (Reduces deposition rate)
Material undergoes many gas collisions
Material can also be deflected straight back onto the target

## Slide 41: Why
Why the mean free path is high at low pressure
B 
A  Current densities are sufficiently high (-1 mAcm-') to make sputtering useful

## Slide 42: Direct current sputtering
Metal deposition rate is high with DC sputtering
The positively charged sputtering gas is accelerated towards target
The ejected atoms get deposited on substrates
Sputtering
gas
DC Power supply
Vacuum
pump
Target
Substrate

## Slide 43: Radio frequency sputtering
v
RF Power supply
The deposition rate is low compare with DC sputtering
In negative half cycle, sputtering gas atoms get attracted by source
In positive half cycle target atoms ejects from the source along with gas atoms and accelerate towards substrate
Target
Substrate
Sputtering
gas
Vacuum
pump

## Slide 44: Diode sputtering
No magnet at the target
Target atoms can move freely in the vacuum chamber
Target atoms are not directly deposited on the substrate
This increases the process time

## Slide 45: Reactive sputtering
Reactive gas is introduced along with argon, It reacts with the target atoms to form the desired compound
Oxygen and nitrogen are commonly used
The process suffers from one important drawback, namely target 'poisoning’
The hysteresis curve obtained when a metal target is sputtered in a reactive gas. As the reactive gas flowrate is increased a sudden transition occurs where the compound forms on the surface of the target. The sputtering rate drops and the partial pressure of reactive gas increases ensuring even further target 'poisoning'

## Slide 46: VSM (Vibrating Sample Magnetometer)
SQUID converts current into voltage
Precise measurement depends on better sample centering
B field
SQUID with electronics
Flux transformer
Detection coil (or) Gradiometer
Sample position
Prepare the presentation
Highly sensitive magnetic moment measure device over a range of (1.8 - 400 K) and (7 T)
Sample magnetic field cuts the winding and detects the gradient in terms of current
Flux transformer boost the flux
Works on basic principle
Of Faraday’s law
Notes: Frequency (?)

## Slide 47: Sample centering
Second-order gradiometer
Magnetic moment
SQUID output
signal
L = Scan length
n = No. of data points
Vi = Voltage reading at ith point
C = Calibration factor
(Current to voltage ratio)
Magnetic Dipole

## Slide 48: Superconducting magnet
Super conducting magnet wounded in solenoid configuration
Heater ON, Super conducting loop is open
Heater OFF, Super conducting loop is closed
Persisting current flows in the circuit
Negligible resistance at less than critical temperature leads, persisting current
Dewar can evacuated and purged with helium gas

## Slide 49: VSM: In-plane rotation
For rotation,
rotate sample clockwise
For rotation,
rotate rod anticlockwise
x
z
M
y
H
z
x
y
M
H
x
y
z
M
H
x
y
z
H
M
x
y
z
H
M
E(,)
E

## Slide 50: VSM: Out-of-plane rotation
For rotation, tilt the sample by using glass pieces
For rotation,
rotate sample
y
z
x
M
H
z
y
x
M
H
z
x
y
H
z
x
M
y
H
x
y
z
H
M
x
y
H
M
z
E(,)
E
Focus on this part

## Slide 51: VSM results

## Slide 52: Piezoelectric
Piezoelectric materials can be polarized by electric field and mechanical stress
Converse piezoelectric effect
Hysteresis of piezoelectric material
Change the figures
Put in introduction chapter
Direct piezoelectric effect :
Converse piezoelectric effect :
Polarized by stress
Polarized by electric field
+
-
+
-
+
-
+
-
+
-
Notes: Poled polarity = Applied voltage polarity for strain  Additional expansion

## Slide 53
Interfacial anisotropy
Bulk
MgO
Interface
z
y
x
CoFeB

## Slide 54: Stress - strain machine
Load cell strain with elongation and compression load
Deformation (strain )of material, when Load (stress ) is applied on it
Chart: Stress vs strain
| 0.2 | 1.1000000000000001 | 5.4 | 10.199999999999999 | 14.3 | 19.5 | 25.8 | 34.6 | 37.799999999999997 | 40 | 43.3 | 47.8 | 51.6 | 54.9 | 58 | 61.7 | 65.599999999999994 | 72.8 | 82.3 | 100 | 128.4 | 156.5 | 188.7 | 222 | 265.8
Stress vs Strain | 0 | 0.02 | 0.04 | 0.06 | 0.08 | 0.1 | 0.12 | 0.14 | 0.16 | 0.19 | 0.21 | 0.23 | 0.25 | 0.27 | 0.29 | 0.31 | 0.33 | 0.36 | 0.38 | 0.4 | 0.42 | 0.44 | 0.46 | 0.48
Load cell
Young’s modulus

## Slide 55: Strain gauge
Senses material contraction and elongation in terms of resistance
when material is influenced by an external force
Triaxial strain gauge
Wheatstone bridge circuit to measure the resistance
  (
Notes: Ks = gauge factor (2.1)

## Slide 56: Electromagnet
Current carrying conductor produce magnetic field around it
Hall probe converts the magnetic field into Hall voltage
Magnetizing the magnetic sample by varying theta with temperature
Magnetic thermal annealing
Electromagnet
Flux = No. of turns * input current

## Slide 57: Magnetic thermal annealing
Thermal annealing setup
Electromagnet
Constant current controller
Chiller
Vacuum
pump
Heater
Pirani gauge
0.01 mbar
PC
Sample
stand
Magnetic thermal annealing at 400mT, 400 degrees for 1 hour
Thermometers
S.Ikeda et al, DOI:10.1038/NMAT2804 (2010)

## Slide 58: Differential amplifier

## Slide 59
THANK YOU

## Slide 60: Magneto-Optical Kerr Effect

## Slide 61: Magnetic force microscopy

## Slide 62: Electrical potential in the neuron
Releasing transmitter molecules  Change in permeability  Change in membrane potential
Excitatory synapse
Inhibitory synapse
Depolarization
Repolarization
Na+ inflow begins
Sufficiently depolarized postsynaptic neurons cause action potential
Concise slide on signal propagation
-
+
Membrane voltage positive for a short time
Na+ inflow ends
K+ outflow becomes dominate

## Slide 64: Electrical potential in the neuron
Releasing transmitter molecules  Change in permeability  Change in membrane potential
Excitatory synapse
Inhibitory synapse
Depolarized membrane Excitatory PSP
Repolarized membrane inhibitory PSP
Depolarization
Repolarization
Na+ inflow ends
K+ outflow becomes dominate
Na+ inflow begins
Sufficiently depolarized postsynaptic neurons cause action potential
Membrane voltage positive for a short time
+
-
Concise slide on signal propagation

## Slide 65: Current in neurons
Current = 1 e-6 A
Radius = 100 e-6 m
Direction of propagation
Volume current (?)
Ohmic current (?)
Currents: Bidirectional movement of ions due to chemical gradient at membrane
Primary current: Movement of ions due to chemical concentration gradient
Volume current: Completes loop of ionic flow, so that no buildup of charge on membrane
Action potential
Equilibrium membrane
-
+
Notes: Positive ions flows along the direction of propagation  Inside the neuron  Ohmic currents flow along the propagation
Relatively Negative ions flows along the direction of propagation  Outside the neuron  Volume currents flow opposite the propagation

## Slide 66: Sputtering
Sputtering is a technique to deposit metals/Insulators on a substrate
Plasma is created at high voltage under high vacuum
Deposition can be controlled by SCCM (standard cubic centimeter per minute) of Ar+ gas
DC sputtering - Metal deposition
RF sputtering - Insulator deposition
Argon gas
Vacuum pump
v
Targets
Improve the slide
Include vacuum pump
Chamber pressure 10e-9 mbar

## Slide 67: Sputtering
Sputtering is a technique to deposit metals/Insulators on a substrate
Magnetron sputtering : Magnet keeps high density of sputtering ions leads higher efficiency
DC - Metal deposition
RF - Insulator deposition
Argon gas
Vacuum pump
v
Chamber pressure
10e-9 mbar with turbo pump
Cathodic sputtering : Inelastic collision between Ar+ ions and target atoms
High vacuum allows
sufficient mean free path

## Slide 68: Piezoelectric
Piezoelectric materials can be polarized by electric field and mechanical stress
Direct piezoelectric effect :
Converse piezoelectric effect :
Polarized by stress
Polarized by electric field
Converse piezoelectric effect
Hysteresis of piezoelectric material
Change the figures
Add matrix terms
Put in introduction chapter
Notes: Poled polarity = Applied voltage polarity for strain  Additional expansion

## Slide 70: Magnetic thermal annealing
Reorientation of the easy axis in a ferromagnetic material
It reorients each spin along applied magnetic field
Magnetic thermal annealing setup
Totally re-visit the slide
What happens to sample with temperature?
Add arrows ?
Add pump picture and learn different kinds pump ?
Add Vacuum level ?
Add electromagnet chiller pic ?
Add sample holder ?
Add magnetic field, time and temperature ?
Heater
Pirani gauge
Constant current control source
Electromagnet
Thermal anneal chamber

## Slide 71: Magnetic thermal annealing
Reorientation of the easy axis in a ferromagnetic material
It reorients each spin along applied magnetic field
Magnetic thermal annealing setup
Totally re-visit the slide
What happens to sample with temperature?
Add arrows ?
Add pump picture and learn different kinds pump ?
Add Vacuum level ?
Add electromagnet chiller pic ?
Add sample holder ?
Add magnetic field, time and temperature ?

## Slide 72: X-Rays diffraction (XRD)

## Slide 73: Ultrasensitive measurement instruments

## Slide 74
x-axis
y-axis
z-axis
DC sputtering - Metal deposition
RF sputtering - Insulator deposition
Argon gas
Vacuum pump

## Slide 75
Negative (Cathode)
Ground (Anode)
Argon sputtering gas
Vacuum pump
Sputtering target
Substrate

## Slide 76
P
E
H
M
Piezoelectricity
Magnetostriction
Magnetoelectricity (intrinsic)

## Slide 77
P
E
H
M
Piezoelectricity
Magnetostriction
Magnetoelectricity (intrinsic)

## Slide 78: I have done
Wafer cleaning, cutting
I have deposited different magnetic metals by sputtering
Measured the sample thickness in SEM
Magnetized the magnetic sample in out off plane and in plane
Anneal the sample at high temperature
I have generated hysteresis curves of those magnetic sample in VSM
Poled the piezoelectric material (PMN-PT wafer) at high voltage
Observed the piezoelectric voltage with applied stress by machine
Observed the strain vs voltage plots

## Slide 79: Orientation of current dipole Tangential and radial dipole
Current dipole is an equivalent source of electric field and magnetic fields
MEG is sensitive to the tangential current dipole
EEG can sense all orientation of sources
Theoretically radial dipole produce zero magnetic field on out of a spherical shell
Practically, head is not spherical and all orientation of current dipole can generate magnetic field
Electrically active but magnetically silent
Magnetically active but electrically silent
Radial dipole
Tangential dipole

## Slide 80: Currents in neuron
Currents: Bidirectional movement of ions due to chemical gradient
Primary current: Movement of ions due to chemical concentration gradient
Volume current: Completes loop of ionic flow, so that no buildup of charge on membrane
Generated magnetic field is due to both primary and volume currents
Some part of the brain, volume current generate equal and opposite magnetic fields of primary current causes net zero field outside the head (Very complex to understand)
The resultant direction of current flow in neuron is perpendicular to the cortical sheet of grey matter, where the ion diffusion occur
Notes: Passive current :- Current that generates by absence of action potential
Volume current occur mainly during the action potential The current that would be generate to maintain the

## Slide 81
When axon hillock reaches the threshold level, electrical impulses propagate from neuron to neuron
x-axis
y-axis
z-axis
x
y
z
Magnetization
direction
φ

## Slide 82: Action potential_2
Sufficiently depolarized postsynaptic cell causes action potential
When axon hillock reaches the threshold level, electrical impulses propagate from neuron to neuron
Action potential leads membrane voltage positive for a short time
Depolarization
Repolarization
Na+ Inflow ends
K+ Outflow becomes dominate
Na+ Inflow begins
Equilibrium membrane potential -70mV
Notes: A group of sufficiently depolarized postsynaptic cell generate higher potential, that causes action potential and potential at axon hillock aswell
When axon hillock potential reaches the threshold limit, electrical impulses propagate from neuron to neuron

## Slide 83: Neural basis of magnetoencephalography
Pre-synaptic neuron cell body
Post-synaptic neuron cell
Neuron
Cell body (Soma)
Notes: Generally we have two hemisphere and four in our brain,
Two hemisphere separated by longitudinal fissure and communicate by carpus callosum (group of neurons)
Four lobes separated by particular fissure and communicate by the neuron, which have the connection between white matter() and grey matter(occupied by the neurons )
____
This is the neuron with axon and this is the cell body
They are lot of other neuron cells connected to the cell body and shown cell signal receiver called dendrites
Electrical voltages generated in the neuron by the chemical gradient

## Slide 84: Post-synaptic potential (PSP)
Permeability of membrane changes when transmitter molecules released to synaptic cleft arrive at post synaptic cell
Change in membrane potential leads current flows in interior of postsynaptic cell
Opening ion channels through membrane causes flow of ions (K+ , Na+ and Cl-)
Depolarized membrane causes excitatory PSP
Repolarized membrane causes inhibitory PSP
Neuro transmitter molecules
Synaptic cleft (50 nm)
Receptor channels
Dendrites
Excitatory synapse
Inhibitory synapse
Notes: Change in membrane potential follows permeability of membrane, permeability change when transmitter molecules released into synaptic cleft
This molecules flow, it arrives at post synaptic cell (Which is dendrites), the receptor channels receive the transmitter molecules this leads electric field and current in flow in interior of postsynaptic potential
Neuro transmitter molecule get membrane depolarize and repolarize, it causes the excitatory synapse and inhibitory synapse

## Slide 85: Action potential
Action potential
Equilibrium membrane
-
+

## Slide 86
Tangential dipole are magnetically active but electrically silent
Radial dipole are electrically active but magnetically silent
T
R
Practically, head is not spherical and all orientation of current dipole can generate magnetic field
Theoretically radial dipole produce zero magnetic field on out of a spherical shell

## Slide 87: Vibrating Sample Magnetometer (VSM)
θ=0o
H
M
z
y
x
In-plane sample
z
y
x
Perpendicular sample
θ=0o
H
M
For Փ variation, rotate rod in anti-clockwise
For θ variation rotate sample in clockwise direction
For θ variation tilt the sample by using glass pieces
Notes: Magnitude of a circulation of electric field around a closed loop is equal to the rate of change of the magnetic flux through the are enclosed by the loop.

## Slide 88: In-plane _ OK
In-plane theta = 0-180o, phi = 90o
comes when theta = 90o
In-plane phi = 0-360o at theta = 90o
y- axis
z- axis
x- axis
z- axis
x- axis
y- axis
Position shows theta = 0o
Position shows phi = 0o

## Slide 90: Out-of-plane _ OK
y- axis
z- axis
x- axis
Out of-plane theta = 0-180o, phi = 0o
comes when theta = 90o
y- axis
x- axis
-z- axis
Out of-plane phi = 0-360o
at theta = 90o
Position shows theta = 0o
Position shows phi = 0o

## Slide 92: Magnetic thermal annealing
Lattice deformities can degrade material quality
It helps to eliminate structural imperfections
Reorientation of the easy axis in a ferromagnetic material
It reorients each spin along applied magnetic field, if the sample has deformed ferromagnetic lattice
Magnetic thermal annealing setup

## Slide 93: Magnetic thermal annealing
Temperature rise time = 20-30 min
Electromagnet run time_1 = 30 min
Electromagnet off time = 50 min
Electromagnet run time_2 = 30 min
Temperature fall time = 20-30 min

## Slide 94
PZNPT – Lead zinc niobate lead titanate
PMNPT – Lead magnesium niobate lead titanate
1T=1e4 Oe, 1pT=1e-8 Oe,
3500 Oe - 6 kV
1e-8 Oe – 1.7e-8 kV
V = E*d = 1.7e-8 kV * 0.3 cm = 0.51e-8 = 5 nV

## Slide 96: Sputtering
Thermal evaporation  Solids to vapors
Cathodic sputtering  Inelastic collision b/w Ar ions and target atoms
Magnetron sputtering  Magnet keeps high density of sputtering ions leads higher efficiency
Pulsed laser deposition  laser directed at the target to vaporize the target material.
Reactive sputtering  Plasma is activated by reactive gas
Target is negative
Substrate is positive
Argon gas is positive
Magnetron sputtering  Magnet keeps high density of sputtering ions leads higher efficiency
High vacuum allows sufficient mean free path
The average kinetic energy of the ejected atoms depends on the energy, angle and type of incoming ion, and the nature of the target material, and is typically tens of eV.
Notes: Elastic collision = KE1=KE2 and P1=P1
Inelastic collision = KE1 not equal KE2 and P1=P2

## Slide 98: Questions…
Electric field is zero in side the conductor ?
Piezoelectric material d=SE and measurements
Hysteresis single domain and multi domain ()
COMSOL simulation (Point charge done)
Difference between synapses and dendrites
Does the magnitude and direction

## Slide 99: To-do
Ac response and units ft/cm--------AC signal
Second Maxwell eq. 2--------------4th eq
Detail understand on neural and signal transmitter------- synapse and receptor
diffusion eq.
install mat lab
P(k)-------------------
post synaptic equations
what is synaps------signal t/f neuron to neuron
Latex-------------
MEG writeup
Sputtering writeup
Matlab package for maxwell
Need to draw own figures
Matlab file upload (m.file)
Use comsol fig. 4(a) and upload
Get comsol table for point source
Focus on INVERSE PROBLEM
Work on Differential AMPLIFIER with Anurag

## Slide 100: To do
Remember UNITS of permittivity (faraday/meter), permeability(H/meter)
MEG in Epilepsy
Why do we need to measure gradient in space of magnetic field?
Write a program that can generate Gaussian signal and its derivative as in Fig. 27
Generate a signal with noise and apply averaging filter for smoothing
Read all about white noise
Understand noise co-relation
Understand Fig. 32
Understand sampling neuro magnetic signal
Understand interpolation
Put things in LATEX and discuss
Do line segment in COMSOL
Change the picture in motivation

## Slide 101: Current- To do
Understand: Units ft/cm
Understand: Goldman’s equation
MEG presentation: Inverse problem, Noise (moving average filter)
Difference between synapses and dendrites
Slides
    Add magnetostriction slide (added)
    Piezoelectric simulation
    COMSOL simulation - current dipole figures 4 and 5, Generate figures 19, 24 and 25
    Strain guage
    Get interface anisotropy slide from priyesh
    Calculation on sensor (output 5nV) – Take from khritish (added)
    Magnetic thermal annealing
    Gauss meter

## Slide 102: Current - To do
Magnetic shielded chamber
    How magnetic shielded room cancels the magnetic field ?
Sputtering
    DC sputtering – insulation deposition ?
    Working principle ?
    What is plasma, different colors of plasma ?
    RF magnetron sputtering ?
    Units of vacuum, rotary and turbo pump
    Reactive sputtering ?
    Confocal sputtering ?
  Magnet
    Sensor has single domain (or) multi domain magnet ?
  Stress strain machine
    Units of Young's modules (Neuton/m2) ?
    Poling condition ?
    Different types of load cell, why S type (symmetrical expansion and contraction on both sides )and where to paste the sample ?
    Why we need to paste the sample on top of load cell if pooling is along thickness ?

## Slide 103: Current –To-do
Strain gauge
  Resistance of the wire ?
  Value of gauge factor and how to calculate ?
  Gauge factor equation (
  ?

## Slide 104
Glass pieces height
Sputtering slides
Understand point charge in COMSOL
Pooling for 30 min at maximum voltage

## Slide 105: Q&A
How do you make sensor ?
Vacuum level of sputtering machine and units ?
Why argon gas is used in sputtering ?
What is dendrites ?
How the signal propagate in neuron ?
Membrane of neuron – semi permeable membrane ?
How the diffusion process continues ?
Action potential and post synaptic potential _ Understand the equations ?
How to detect the abnormal activity of the neuron from measured signals ?
Present techniques to measure voltage from head and how your method is different from that ?
Potential divider ?

## Slide 106: Q&A
Why electric field is zero in side conductor ?
Continuity equation ?
Why 1.3 nm ?

## Slide 107
How does a signal propagate through neuron ?
Activation function in neuron ?
How do we understand the weights and bias in neuron ?
Does threshold voltage depend upon the synaptic cleft ?
Ft/cm understand the units
Do we need lithography for designing the sensor ?
Understand gauss probe axial and transverse ?

## Slide 108: Tomorrow work
How do the signals propagate in a neuron ?
  Weighted bias in biological neuron ?
Think about magnetic shielded room ?
  How to measure earth magnetic fields ?
  How do earth magnetic field cancels ?
Magnetic thermal annealing- slide ?
Send sputtering targets and silicon samples to Indore PMN-PT, PZT and FeGa ?
Open vacuum desiccator get 2nm CoFeB sample for VSM ?
  Clean the vacuum desiccator top surface
  Check whether the resistance is fluctuating or not before VSM ?
  Anneal the sample at 500 degrees for an hour
  Check the resistance whether it is constant now ( Priyesh )
  Record the resistance in data sheet
  Do VSM
  Do magnetic thermal annealing
  Do VSM again
Afternoon work on piezoelectric characterization ?
  Measure the strain before poling
  Observe the strain of the piezoelectric wafer before pasting on load cell
  Paste the wafer on load cell with glue
  Observe the strain again
  Apply the stress and note
How to depolarize the piezoelectric material and demagnetize the magnetic material ?

## Slide 109: Thumb rules
Do not put any thing in slide, that you can not explain

## Slide 110: Experimental to-do
Update the procedure on load cell with strain gauge