## Slide 1: Energy-Efficient Neuromorphic Computing
Khritish Kumar Behera 17125
Mail: khritish17@iiserb.ac.in
Indian Institute of Science Education and Research [IISER] Bhopal
Advisor: Dr. Kuntal Roy
Mail: kuntal@iiserb.ac.in
MS Project: Final Presentation
Date: 27-04-2022

## Slide 2: Content
Recap
Motivation
Artificial Neural Network
Character Recognition Model
Spintronics
Magnetic Anisotropy
Magneto-elastic Anisotropy
Perpendicular Anisotropy
Giant Magneto-Resistance
Tunneling Magneto-Resistance
Multiferroic Composites
Ferromagnetic Resonance
Experimental
Ferromagnetic Resonance Setup
Sputtering Plan
MgO/CoFeB MOKE Result
Neuromorphic hardware
Future Works

## Slide 3: Content
Recap
Motivation
Artificial Neural Network
Character Recognition Model
Spintronics
Magnetic Anisotropy
Magneto-elastic Anisotropy
Perpendicular Anisotropy
Giant Magneto-Resistance
Tunneling Magneto-Resistance
Multiferroic Composites
Ferromagnetic Resonance
Experimental
Ferromagnetic Resonance Setup
Sputtering Plan
MgO/CoFeB MOKE Result
Neuromorphic hardware
Future Works

## Slide 4: Energy-Efficient Neuromorphic Computing
Spintronic devices encapsulates
Weight, Sum and Threshold function
Spintronic devices can be more energy-efficient than traditional transistors
Neuromorphic Computing is usually performed on traditional transistor based devices
Non-Boolean Computing
Magnetostrictive
Insulator
Write
Read
.
.
.
Neuron
Piezoelectric

## Slide 5: ANN: Sequential Process
b
Summation
Activation
Non-linear function
b
Weight, strength of the edge
Bias, sets the activation function
Inspired from biological neuron

## Slide 6: Artificial Neural Network: Neural Architecture
Input
35 (7x5)-bit word of the test character
Output
26-bit word suggesting the character
Input
A: 01110 10001 10001 11111
10001 10001 10001
Output
A: 10000000000000000000000000
B: 01000000000000000000000000

## Slide 7: Spintronics: Spin-Electronics
Electron
Spin
Spin
UP
DOWN
Bits
0
1
Spintronic devices, advantages over transistor
  non-volatile
  endurable
There are no charge movement, only spin rotation
  No Ohmic , dissipation
  Dissipation due to magnetization damping
  Dissipation due to applied external charge voltage/current
Electron Beam Lithography
Charge

## Slide 8: Magnetic Anisotropy
CoFeB
Ellipsoid
Sphere
Elliptical Cylinder
In-plane
Shape anisotropy
No anisotropy
Difficult to fabricate
z
y
Magnetization
x
Volume
Coercive field
M
H
Hk
30-80 KT at 300 K
KT,
10 years data retention time

## Slide 9: Magneto-elastic anisotropy
Magnetostrictive Materials: Certain ferromagnetic specimen changes its shape (strain:) during the process of magnetization
Magnetostriction Co-efficient
Magnetic Anisotropy
Stress Anisotropy
Cobalt:
FeGa:

## Slide 10
Giant Magneto-Resistance (GMR)
A. Fert, M.N Baibich et al., Phys. Rev. Lett. 61, 2472 (1988)
P. Grunberg, G. Binash et al., Phys. Rev. B 39, 4828 (1989)
Giant Magneto-Resistance (GMR)
1988

## Slide 11
Tunneling Magneto-Resistance (TMR)
Conductance is proportional to the density of states
NL↑, NR↑, NL↓, NR↓
Julliere, M. Tunneling between ferromagnetic film. Phys. Lett. A 54, 225-226 (1975)
Moodera, J. S. et al., Phys. Rev. Lett. 74, 3273 (1995)
Mathon, J. et al., Phys. Rev. B 63, 220403 (2001), Butler, W. et al., Phys. Rev. B 63, 054416 (2001)
Yuasa, S. et al., Nature Mater. 3, 868 (2004), Parkin, S. et al., Nature Mater. 3, 862-867 (2004)
Reported 1975 (prior to GMR)
TMR>500% using MgO spacer
Insulator
e.g., Al2O3, MgO
Left (L)
Right (R)
Left (L)
Right (R)

## Slide 12: Multiferroic Composites
P
E
H
M
Piezoelectricity
Magnetostriction
Magnetoelectricity (intrinsic)
Multiferroics
  Room-temperature operation
  Weak magnetoelectric coupling
Piezoelectric
Strain
Magnetostrictive
Multiferroic Composite

## Slide 13: Multiferroic composites Voltage vs stress anisotropy
Y: Young’s modulus
strain transfer
Magnetostrictive layer
with high
Choose piezoelectric layer with high de-coefficient
Stress Anisotropy (for FeGa):
(max.)
Vin
tpiezo
Piezoelectric
Magnetostrictive
PMNPT
FeGa

## Slide 14: Ferromagnetic Resonance
precession
damping
Negative damping to keep the magnetization rotating
Transverse AC field
)
In-plane FMR
Perpendicular FMR
LL Equation

## Slide 15: Ferromagnetic Resonance
precession
damping
Lorentzian
FMR absorption is given by the imaginary part
At
LL Equation
Derivative FMR spectra
15
FMR linewidth
Half width at half maximum (HWHM)

## Slide 16: Content
Recap
Motivation
Artificial Neural Network
Character Recognition Model
Spintronics
Magnetic Anisotropy
Magneto-elastic Anisotropy
Perpendicular Anisotropy
Giant Magneto-Resistance
Tunneling Magneto-Resistance
Multiferroic Composites
Ferromagnetic Resonance
Experimental
Ferromagnetic Resonance Setup
Sputtering Plan
MgO/CoFeB MOKE Result
Neuromorphic hardware
Future Works

## Slide 17: Measurement automation with LabView : Electromagnet
Creates a session with electromagnet’s controller for communication
Takes current as input, to set it in the electromagnet
Measures the magnetic field using the gauss probe
Terminates the session and stops further communication
Electromagnet
Gauss probe
Controller
PC with labview is connected to the controller
The gauss probe and the electromagnet is also connected to the controller

## Slide 18: Measurement automation with LabView : RF Signal Generator
Creates a session with RF signal generator for communication
Configures the RF signal frequency
Configures the RF signal power level
Configures ON/OFF state of the signal generator
Terminates the session with RF signal generator
PC with labview is connected to the RF signal generator

## Slide 19: Measurement automation with LabView : Spectrum Analyzer
Creates a session with spectrum analyzer for communicat-ion
Configures the spectrum analyzer
Fetch the trace from the device
Search position on trace to put marker
Retrieves data from the marker
Terminat-es the session with the device
PC with labview is connected to the Spectrum analyzer

## Slide 20: Measurement automation with LabView : Spectrum Analyzer
PC with labview is connected to the Lock-in amplifier
Creates a session with lock-in amplifier for communicat-ion
Sets the input signal parameters
Configures the internal oscillator for reference signal
Configures the sensitivity
Configures the time constant and low pass filter slope
Terminates the session with lockin

## Slide 21: Ferromagnetic Resonance: Experimental Setup
Controller
Laptop with LabView
Spectrum Analyzer
Signal Generator
Electromagnet
Coplanar Waveguide
From Signal Generator
To Spectrum Analyzer

## Slide 22: Ferromagnetic Resonance: Experimental Setup
PC with LabView
RF Signal Generator
S
Sample
Spectrum Analyzer
Co-planar waveguide
Electromagnet
From Signal Generator
To Spectrum Analyzer

## Slide 23: Ferromagnetic Resonance: Result

## Slide 24: Ferromagnetic Resonance: Experimental Setup
PC with LabView
RF Signal Generator
S
Sample
Lock-in Amplifier
Co-planar waveguide
Electromagnet
From Signal Generator
Schottky diode
Helmholtz Coil

## Slide 25: Sputtering Plan
Kapton
PMN-PT
Kapton
PMN-PT
FeGa
Thin-film 1
Thin-film 2
PMN-PT thickness
  25, 50, 75, 100 nm
Dielectric coefficient
Young’s modulus
Poisson ratio
P-E hysteresis
PFM
PMN-PT thickness
  25, 50, 75, 100 nm
FeGa thickness
  0.8, 1, 1.2, 1.5, 1.7, 2, 5, 10, 20, 50, 100 nm
FMR, VSM, MOKE
Four-Probe, MFM

## Slide 26: Sputtering Plan
Kapton
PMN-PT
FeGa
or GGG
CoFeB
MgO
CoFeB
Ta
Ru
Cr/Au
Thin-film 3
Thickness
  PMN-PT: 50 nm
  FeGa: 2 nm
  : 40 nm
  CoFeB (bottom): 2 nm
  MgO: 0.8 nm
  CoFeB (top): 3 nm
  Ta: 5nm
  Ru: 5 nm
  Cr/Au: 100 nm
TMR
TMR measurement

## Slide 27: Sputtering Plan
Kapton
PMN-PT
FeGa
MgO
CoFeB
Ta
Ru
Cr/Au
Thin-film 4
Thickness
  PMN-PT: 50 nm
  FeGa: 2 nm
  MgO: 0.8 nm
  CoFeB (top): 3 nm
  Ta: 5nm
  Ru: 5 nm
  Cr/Au: 100 nm
Kapton
PMN-PT
FeGa
MgO
CoFeB
Thin-film 5
TMR
MFM
Four-probe
TMR measurement
MFM, Four-probe measurement

## Slide 28: MOKE: MgO/CoFeB
Chart: CoFeB_10nm sample
Chart: CoFeB_20nm sample
Si/Ta(5)/MgO(0.8)/CoFeB(10)
Si/Ta(5)/MgO(0.8)/CoFeB(20)

## Slide 29: Neuromorphic hardware
Magnetostrictive
Insulator
Write
Read
MTJ
Piezoelectric
Single Neuron
Single/multiple input is given to the piezoelectric layer
Piezoelectric material acts as summation block
Blue pillars are of different size, it encapsulates weight
Number of pillars depends on the number of other neurons connected

## Slide 30: Neuromorphic hardware
Artificial neural network
Neuromorphic hardware

## Slide 31: TMR calculation
The stress anisotropy affects the energy barrier of TMR
Parallel or anti-parallel orientation
Resistance area product for parallel orientation
TMR=200%
TMR =
If constant current, applied, on TMR of dimension nm
  mV
  mV
W=1
W=0
TMR, orientation
Encapsulating the weight between / and

## Slide 32: What I have done
 | TASK | ECS501 | 
 |  | MID-TERM | END-TERM
1 | Character recognition model implementation |  | 
2 | Magnetic thermal annealing |  | 
3 | Different experimental apparatus |  | 
4 | LabView for automation of different devices |  | 
 | TASK | ECS502 | 
 |  | MID-TERM | END-TERM
1 | Electron beam lithography patterning |  | 
2 | Ferromagnetic Resonance setup in lab |  | 
3 | LabView for automation |  | 
4 | Worked on Lockin-Amplifier |  | 

## Slide 33: What I have done
 | TASK | ECS502 | 
 |  | MID-TERM | END TERM
1 | Sputtering plan |  | 
2 | Neuromorphic hardware design |  | 
3 | MgO/CoFeB deposition |  | 
4 | MOKE characterization of MgO/CoFeB |  | 

## Slide 34: Future Works
 | TASK
1 | Electron beam lithography
2 | Sputtering
3 | VSM, FMR, MFM, PFM, TMR characterization

## Slide 35
?
Thank You

## Slide 36: EBL Patterning

## Slide 37: What I have done
LabVIEW automation
Spin coating
EBL patterning
Sputtering and plans
Character recognition model
Helmholtz coil some results
Lock-in amplifier
VSM
  Magnetic thermal annealing
MOKE
  MgO/CoFeB data
  XRR of MgO/CoFeB
TMR
  Four probe
FMR
  Experimental setup
  Result
  Schottky diode results

## Slide 38: Content
Recap
Motivation
Artificial Neural Network
Character Recognition Model
Spintronics
Magnetic Anisotropy
Magneto-elastic Anisotropy
Perpendicular Anisotropy
Giant Magneto-Resistance
Tunneling Magneto-Resistance
Multiferroic Composites
Ferromagnetic Resonance
Experimental
Ferromagnetic Resonance Setup
Sputtering Plan
MgO/CoFeB MOKE Result
Device Architecture
Future Plan

## Slide 39: What I have done
Built a character recognition model using artificial neural network in MATLAB
Worked on magnetic thermal annealing for better magnetic hysterisis
Learned all the small instruments like spin coater, ultrasonic cleaner, shaker, hot plate, hot air oven, rota mantle, nitrogen gun, vacuum desiccator, muffle furnace, fume hood, source measuring unit, power supply, probe station, oscilloscope
Did the LabVIEW automation of power supply, signal generator, spectrum analyzer, electromagnet and lock-in amplifier
Built a co-planar waveguide for FMR setup
Designed the FMR setup and automated it with electromagnet, signal generator, spectrum analyzer
Did the EBL patterning for deposition of PMN-PT and FeGa nano-structure
Did spin coating of photo resist on Si 3x1.5mm wafer of 100nm thickness

## Slide 40: What I have done
Learned wafer cleaning process
Read the perpendicular anisotropy paper
Did sputtering deposition of CoFeB/Pt materials and the plans for thin film deposition of PMN-PT, FeGa, MTJ
Measured the magnetic field between the two poles of the electromagnet
Measured the current generated by placing 90 turns of Cu coil in magnetic field
Measured the magnetic field when constant current flows in 90 turns of Cu coil
Worked on lock-in amplifier
Did the Schottky diode AC rectification at higher frequency
Measured the M-H hysteresis of MgO/CoFeB in MOKE
Measured the XRR values of MgO/CoFeB
Designed the neuromorphic hardware architecture

## Slide 41: Content
Recap
Motivation
Artificial Neural Network
Character Recognition Model
Spintronics
Magnetic Anisotropy
Magneto-elastic Anisotropy
Perpendicular Anisotropy
Giant Magneto-Resistance
Tunneling Magneto-Resistance
Neural network using spintronics
Multiferroic Composites
Proposed Device
Experimental
Measurement Automation with LabView
Ferromagnetic Resonance
  Electromagnet
  RF Signal Generator
  Spectrum Analyzer
Lock-in Amplifier
Schottky Diode
Future Plan

## Slide 42: Content
Recap
Motivation
Artificial Neural Network
Character Recognition Model
Spintronics
Magnetic Anisotropy
Magneto-elastic Anisotropy
Perpendicular Anisotropy
Giant Magneto-Resistance
Tunneling Magneto-Resistance
Neural network using spintronics
Multiferroic Composites
Proposed Device
Experimental
Measurement Automation with LabView
Ferromagnetic Resonance
  Electromagnet
  RF Signal Generator
  Spectrum Analyzer
Lock-in Amplifier
Schottky Diode
Future Plan

## Slide 43: Measurement automation with LabView
LabView
Graphical programming environment
Control and synchronize different devices from different companies
Centralized system for data acquisition

## Slide 44: Ferromagnetic Resonance
precession
damping
Lorentzian
FMR absorption is given by the imaginary part
At
LL Equation
Derivative FMR spectra
44
FMR Signal

## Slide 45: Lock-in Amplifier
Signal
  Amplitude
  Frequency
Good amplifier noise
Bandwidth
Gain
Signal
Noise
PSD in Lock-in amplifier can detect the signal at with bandwidth as narrow as

## Slide 46: Lock-in Amplifier
X
S
X

## Slide 47: Lock-in Amplifier
X
S
X
High frequency component
DC component

## Slide 48: Lock-in Amplifier
X
S
X
DC component
In-phase
Quadrature
LPF
LPF

## Slide 49: Lock-in Amplifier

## Slide 50: Schottky Diode

## Slide 51: Proposed Device
Magnetostrictive
Insulator
TMR
Piezoelectric
.
.
x1
x2
xn
Electric Potential to Piezoelectric
Stress anisotropy in Piezoelectric
Stress anisotropy in Magnetostrictive
Magnetic anisotropy in Magnetostrictive
Inhibits the TMR
Generation of variable voltage
The piezoelectric material
  Serves the purpose of summation
The different dimension of blue pillars
  Serves the purpose of weight

## Slide 52: Perpendicular interface anisotropy
Ikeda, S. et al. "A perpendicular-anisotropy CoFeB–MgO magnetic tunnel junction."
Nature Materials 9 (2010) 721-724
Interfacial anisotropy
Bulk
MgO
Interface
z
y
x
CoFeB
In-plane
sample
Out-of-plane
sample

## Slide 53: Perpendicular Anisotropy
CoCrPt
Bulk
tCoFeB<1.3 nm
CoFeB
MgO
Interface
IISER Bhopal
Circular cross-section
Easy axis:
Magnet’s plane:
Hard axis:
z
y
x
x
y
z
Magnetization
direction
Notes: There are 2 kind of possibilities: Bulk anisotropy and Interface anisotropy
Where Nd(teta, phi) comes form -> spherical coordinate system
What is the requirement for perpendicular anisotropy

## Slide 54: Artificial Neural Network (ANN)
System of interconnected neurons
ANN Architecture
Output of a neuron, connected to all other neurons in the next layer
Three layers: Input, Hidden and Output layers
Weights and biases are the optimizing parameters
Input layer
Hidden layer
Output layer
b

## Slide 55: Ferromagnetic Resonance

## Slide 56: Schottky Diode

## Slide 58: Ferromagnetic Resonance
precession
damping
In-plane FMR
)
Perpendicular FMR
For linearized small rotation
In-plane FMR

## Slide 59: Ferromagnetic Resonance
precession
damping
Negative damping to keep the magnetization rotating
Transverse AC field
Lorentzian

## Slide 60: Ferromagnetic Resonance
precession
damping
Transverse AC field
Derivative FMR spectra
FMR linewidth
Half width at half maximum (HWHM)
FMR Signal
Hdc

## Slide 61: Ferromagnetic Resonance: Experimental Setup
Spectrum Analyzer
Signal Generator
Gaussmeter
Electromagnet
Lab Laptop
Gauss probe
Co-planar waveguide
I/P from Signal Generator
O/P to Spectrum Analyzer

## Slide 62: Ferromagnetic Resonance: Experimental Setup
COIL 1
COIL 2
S
PC with LabView
Spectrum Analyzer
RF Signal Generator
Electromagnet
Lockin-Amplifier

## Slide 63: Lock-in Amplifier
For retrieving signals buried in noise
  Noise to signal ratio is high
  Amplifying signal, amplifies noise
X
High frequency component
DC component

## Slide 64: Lock-in Amplifier
Signal
Noise
500
600
Hz
PSD
0
100
Hz
1000
High frequency
component
DC
component
Trade off:
low cut-off frequency, higher settling time